Crystal structure parameters for deh265: Red blocks; C114H94B2FeN3P3 1676.30 g/mol, monoclinic, space group P21/c ; a = 15.2667(14) Å, b = 15.9297(14) Å, c = 40.090(4) Å, α =  γ = 90°, β = 99.585(3)°; V = 9613.5(15) Å3; Z = 4, calcd = 1.158 g cm−3; crystal dimensions 0.300 x 0.280 x 0.080 mm; 2θmax = 47.036°; 168875 reflections, 14172 independent (Rint = 0.0920), intrinsic phasing; absorption coeff (μ = 0.256 mm−1), absorption correction semi-empirical from equivalents (SADABS); refinement (against Fo2) with SHELXTL V6.1, 1111 parameters, 0 restraints, R1 = 0.1071 (I > 2σ) and wR2 = 0.2484 (all data), Goof = 1.162, residual electron density 0.83/−0.80 Å−3. SQUEEZE was used for two equal solvent voids of 771.9 Å3, 167.6 electrons each.